## Slide 1: AKTIVNA VIŠESLOJNA POLIMERNA AMBALAŽA ZA PAKIRANJE HRANE
Dr. sc. Ana Rešček
PIK Vrbovec-mesna industrija d.d., ana.rescek@pik-vrbovec.hr
26.11.2014.
Hotel Sheraton, Zagreb
Prof. dr. sc. Zlata Hrnjak-Murgić, Fakultet kemijskog inženjerstva i tehnologije, Zagreb
Dr. sc. Ljerka Kratofil Krehula, Fakultet kemijskog inženjerstva i tehnologije, Zagreb
Doc. dr. sc. Anita Ptiček Siročić, Geotehnički fakultet, Varaždin
Međunarodno savjetovanje
Polimerni materijali i ambalaža

## Slide 2: Polimerni ambalažni materijali
AMBALAŽA
ZA
PAKIRANJE
HRANE
MEHANIČKA
SVOJSTVA
OPTIČKA
SVOJSTVA
TERMIČKA
SVOJSTVA
EKOLOŠKA
PRIHVATLJIVOST
BARIJERA
NA AROMU
BARIJERA
NA VODENU
PARU
BARIJERA
NA PLINOVE
(O2, CO2)
ZDRAVSTVENA
ISPRAVNOST
ANTIMIKRO-
BIOLOŠKA
ZAHTJEVI PREMA POLIMERNIM AMBALAŽNIM MATERIJALIMA ZA PAKIRANJE HRANE

## Slide 3
Pravilnim izborom pojedinih slojeva monomaterijala dobije se laminat čija svojstva najbolje odgovaraju određenoj robi i zahtjevima tržišta uz minimalnu cijenu.
Višeslojna polimerna ambalaža
BENEFITI
Poboljšana barijerna svojstva (na O2, CO2, H2O(v), arome...)
Poboljšana svojstva na UV i VIS zračenje
Poboljšana toplinska svojstva
Smanjenje mase ambalaže po jedinici površine
Postupci koji se primjenjuju za dobivanje višeslojnih polimernih materijala su koekstrudiranje i kaširanje

## Slide 4: Barijerna svojstva
POLIMERNI FILM
Propusnost (q) Barijerna svojstva
permeacije malih molekula plinova (O2, N2, CO2 ili H2O(v)) kroz polimerni film

## Slide 5: Barijerna svojstva
I Fickov zakon
II Fickov zakon
Sorpcija ili
koeficijent toplljivosti (S)
P = D ∙ S
Propusnost (q)
q =
Koeficijent permeacije (P)
S =
c = gradijent koncentracije
x = debljina polimernog filma
D = koeficijent difuzije
c = konc. permeacijske tvari
kod ravnotežnih uvjeta
p = parcijalni tlak
- ravnotežno stanje sistema
D = koeficijent difuzije
d = debljina polimera
Jx

## Slide 6
Barijerna svojstva polimera
PROPUSNOST NA PLINOVE I VODENU PARU
NISKO BARIJERNI
Polietilen niske gustoće (LDPE)
Polistiren (PS)
Polietilen visoke gustoće (HDPE)
Polipropilen (PP)
Orijentirani polipropilen (OPP)
Poliamid (PA)
Poli(viniliden-klorid) (PVDC)
Poli(etilen-tereftalat) (PET)
SREDNJE BARIJERNI
VISOKO BARIJERNI

## Slide 7
Aktivna ambalaža
Sadrži ciljane aktivne tvari koje ambalaži daju specifično funkcijsko svojstvo jer mogu apsorbirati tvari iz hrane ili njezine okoline u ambalažu i tako produljiti njezin vijek trajanja.
Aktivne tvari su:
apsorberi O2,
apsorberi CO2
apsorberi H2O(v)
Primjena:
višeslojni polimerni filmovi
polimerni (nano)kompoziti
hrana
hrana

## Slide 8
Kemijski na sebe vežu O2 – znatno usporavaju njegovu permeaciju kroz film vezanjem na površini te usporavaju reakcije oksidacije hrane
Fe → Fe2+ + 2e−
O2 + H2O + 2e− → 2OH−
Fe2+ + 2OH− → Fe(OH)2
Fe(OH)2 + O2 + H2O → Fe(OH)3
Primjena aktivnih nanočestica
APSORBERI KISIKA
nanočestice metala i metalnih oksida
APSORBERI VODENE PARE
2Al2O3 (s) + 6H+ (aq) -> Al3+ (aq) + 3H2O (l)
2Al2O3 (s) + 2OH- (aq) -> AlO2- (aq) + H2O (l)
aluminijev oksid

## Slide 9
Zdravstvena ispravnost ambalaže
PRETPOSTAVKA: 1 kg hrane upakirano u ambalažu površine od 6 dm²
EU 10/2011
„Bilo koji materijal koji dolazi u dodir s hranom mora biti prikladan i neaktivan kako bi se izbjegla migracija tvari u proizvode u količinama štetnim za ljudsko zdravlje te s ciljem smanjenja neprihvatljivih promjena u sastavu i svojstvima hrane.”
Zakonom o plastičnim materijalima i predmetima koji dolaze u neposredan dodir s hranom (NN 25/2013) obuhvaćene su:
EU 450/2009
Uredba o aktivnim i inteligentnim materijalima i predmetima koji dolaze u dodir s hranom
Globalna migracija (GM)
Specifična migracija (SM)
30 mg/kg
60 mg/kg (10 mg/dm2)

## Slide 10: Polietilen niske gustoće, LDPE
Najzastupljeniji polimerni ambalažni materijal → 32,5 %
Primjena:
  ambalažni materijal za prehrambene, farmaceutske, tekstilne proizvode,
  sloj za varenje kod višeslojne ambalaže,
  vrećice za smrzavanje, čepovi, poklopci za boce...
−[CH2 − CH2 ]n−
Nedostatak NISKA BARIJERNA SVOJSTVA
Prednost dobra mehanička i toplinska svojstva, lako se
oblikuje, niska cijena

## Slide 11: Polikaprolakton, PCL
Biorazgradljivi poliester na bazi nafte
  Razgradnja pomoću prirodnih mikroorganizama
  60-90 % otpadnog materijala razgradi se tijekom 60 do 180 dana.
Amorfan na sobnoj temperaturi
Fleksibilan
Kompatibilan s većim brojem polimera
Prednost:
PCL kod višeslojnog filma se biorazgrađuje omogućuje lakše recikliranje
Primjena:
omakšavalo za PVC,
baza za ugradnju raznih dodataka (antioksidansi,
antifugalne, antimikrobne aktivne tvari, boje...)
premazni filmovi
Nedostatak slaba mehanička svojstva

## Slide 12
CILJ RADA
Razvoj novih polimernih materijala za pakiranje hrane s funkcionalnim primjenskim svojstvima.
Utjecaj modificiranih nanočestica na svojstava;
    barijerna,
    mehanička i
    toplinska.
Razvoj aktivne polimerne ambalaže u cilju usporavanja procesa kvarenja i smanjenja količine otpadne hrane.

## Slide 13: METODIKA

## Slide 14
Priprema uzoraka
PRIPRAVA DVOSLOJNIH FILMOVA
Premaz na PE (60 µm) s PCL polimerom s aktivnim tvarima (3 µm)
Disperzija brzinom od 15 000 okretaja/min tijekom 8 min
10 mas % PCL otopina
Aktivne tvari:
  Fe3O4
  Al2O3

## Slide 15
Karakterizacija
Barijerna svojstva
Propusnost na kisik (ISO / DIS 15 105 1), T = 23 °C
Propusnost na vodenu paru (DIN 5333), T = 23 °C
Termogravimetrijska analiza (TGA), b = 10 °C/min, 25-550 °C, N2
Mehanička svojstva, 50 mm/min, T = 23 °C, 65 % r.v.z.
Prekidno istezanje
Prekidna čvrstoća

## Slide 16
REZULTATI

## Slide 17
Uzorak | PCL | Fe
PCL-Fe 05 | 99,5 | 0,5
PCL-Fe 1 | 99,0 | 1
Dvoslojni PE/PCL filmovi s aktivnim tvarima
PCL – polikaprolakton
Fe – Fe3O4
Uzorak | PCL | Al
PCL-Al 1 | 99,0 | 1
PCL-Al 5 | 95,0 | 5
PCL-Al 10 | 90,0 | 10
PCL – polikaprolakton
Al – Al2O3
a) Aktivna tvar: Fe3O4 , % w/v
b) Aktivna tvar: Al2O3 , % w/v

## Slide 18
Chart: Propusnost na kisik (cm3m-2d-1bar-1)
| PE | PE/PCL | PE/PCL-Fe 05 | PE/PCL-Fe 1
Propusnost, q | 1290 | 1210 | 1100 | 1090
Rezultati barijernih svojstava
a) Fe3O4
Uzorak | q cm3m-2d-1bar-1 | S cm3m-2d-1bar-1 | D cm2s-1 | P cm3cm-1s-1bar-1 | tL s
PE | 1290 | 2,97*10-2 | 3,02*10-7 | 8,97*10-9 | 19
PE/PCL | 1210 | 2,90*10-2 | 2,90*10-7 | 8,41*10-9 | 20
PE/PCL-Fe 05 | 1100 | 2,52*10-2 | 3,30*10-7 | 8,32*10-9 | 21
PE/PCL-Fe 1 | 1090 | 2,53*10-2 | 3,24*10-7 | 8,20*10-9 | 21

## Slide 19
Rezultati TG analize
a) Fe3O4
427,9 °C
397,1 °C
475,1 °C
465,9 °C
TG
DTG

## Slide 20
Chart: Prekidna čvrstoća (N/mm2)
| PE | PE/PCL | PE/PCL-Fe 05 | PE/PCL-Fe 1
Prekidna čvrstoća (N/mm-2) | 12.9 | 11.9 | 15.5 | 16.5
Chart: 
| PE | PE/PCL | PE/PCL-Fe 05 | PE/PCL-Fe 1
Prekidno istezanje (%) | 533 | 471 | 676 | 569
Rezultati mehaničkih svojstava
a) Fe3O4

## Slide 21
Chart: Propusnost na vodenu paru (g/m2dan)
| PE | PE/PCL | PE/PCL-Al 1 | PE/PCL-Al 5 | PE/PCL-Al 10
Propusnost, WVTR | 34.2 | 31 | 13 | 23.2 | 25.3
Rezultati barijernih svojstava
b) Al2O3
0,1 - 10 g/m2dan za komercijalnu ambalažu u primjeni za suhu hranu

## Slide 22
Rezultati TG analize
b) Al2O3
TG
DTG

## Slide 23
Chart: Prekidna čvrstoća (N/mm2)
| PE | PE/PCL | PE/PCL-Al 1 | PE/PCL-Al 5 | PE/PCL-Al 10
Prekidna čvrstoća (N/mm-2) | 12.9 | 11.9 | 18 | 18.5 | 16.6
Chart: 
| PE | PE/PCL | PE/PCL-Al 1 | PE/PCL-Al 5 | PE/PCL-Al 10
Prekidno istezanje (%) | 533 | 471 | 651 | 727 | 651
Rezultati mehaničkih svojstava
b) Al2O3

## Slide 24
Zaključci
Najbolja barijerna svojstva kod PE/PCL dvoslojnih filmova, tj. smanjenu propusnost na kisik, pokazuje uzorak s najvećom koncentracijom magnetita (PE/PCL-Fe 1).
Barijerna svojstva, tj. smanjena propusnost na vodenu paru PE/PCL dvoslojnih filmova s Al2O3, znatno su poboljšana (i do 60 %) u odnosu na dvoslojne filmove bez aluminijevog oksida (Al2O3).
Mehanička svojstva PE/PCL dvoslojnih filmova znatno su poboljšana za sve uzorke pripremljene s nanočesticama; magnetit i Al2O3. Tako je čvrstoća za PE/PCL-Al 5 uzorak porasla u odnosu na uzorak čistog PE s 12,9 N/mm2 na 18,5 N/mm2, a istezanje s 533 % na 727 %.
Toplinska svojstva PE/PCL dvoslojnih filmova ostala su nepromijenjena dodatkom nanočestica, a na povećanje toplinske postojanosti dvoslojnih filmova značajno je utjecao premazni sloj polimera polikaprolaktona.

## Slide 25
Literatura
M. Kurek, D. Klepac, M. Ščetar, K. Galić, S. Valić, Y. Liu, W. Yang, Gas Barrier and Morphology Characteristics of Linear Low-Density Polyethylene and Two Different Polypropylene Films, Polym. Bull., 67 (2011), 1293-1309.
R.S. Cruz, G.P. Camilloto, A.C. dos Santos Pires, Oxygen Scavengers: An Approach on Food Preservation, InTech, Structure and Function of Food Engineering, (2012), DOI: 10.5772/48453
S.W. Rutherford, Polymer Permeability and Time Lag at High Concentrations of Sorbate, J. Membr. Sci., 183 (2001), 101-107.
T. Hirvikorpi, M. Vaha-Nissi, A. Harlin, M. Karppinen, Comparison of Some Coating Techniques to Fabricate Barrier Layers on Packaging Materials, Thin Solid Films, 518 (2010), 5463-5466.
H. Aloui, K. Khwaldia, M. B. Slama, M. Hamdi, Effect of Glycerol and Coating Weight on Functional Properties of Biopolymer-Coated Paper, Carbohydr. Polym., 86 (2011), 1063-1072.
D.S. Finch, T. Oreskovic, K. Ramadurai, C.F. Herrmann, S.M. George, R.L. Mahajan, Biocompatibility of Atomic Layer-Deposited Alumina Thin Films, J. Biomed. Mater. Res. A., 87A (2008), 100-106.
C. Silvestre, D. Duraccio, S. Cimmino, Food Packaging Based on Polymer Nanomaterials, Prog. Polym. Sci., 36 (2011), 1766-1782.
Arora, G.W. Padua, Review: Nanocomposites in Food Packaging, J. Food. Sci., 75 (2010), 9-43.
J.M. Lagaron, E. Gimenez, M.D. Sánchez-García, M.J. Ocio, A. Fendler, NovelNanocomposites to Enhance Quality and Safety of Packaged Foods, u: Food Contact Polymers, Rapra Technology, Shrewsbury, 2007.
C.F. Struller, P.J. Kelly, N.J. Copeland, Aluminum oxide barrier coatings on polymer films for food packaging applications, Surf. Coat. Tech., 241, 130-137.

## Slide 26
HVALA NA PAŽNJI !